Section 7000  Stalite EXTENSIVE Sedum GREEN ROOF GROWING MEDIA for 4” Depth Mid Atlantic and SE Blend

### PART 1 – GENERAL

- SUMMARY

- Section Includes:

  - Stalite(  Green Roof Growing Media

  - REFERENCES

- ASTM – American Society for Testing and Materials

ASTM E2788-11, ASTM E2397-11, ASTM E2399-11

B.   FLL Guidelines for the Planning, Execution and Upkeep of Green-Roof Sites

# A.  Stalite premixed Extensive Green Roof Growing Media containing the components

# 75% Stalite G Fines: 15% compost: 10% Pine Bark Fines

PART 2 – PRODUCTS

  - ACCEPTABLE MANUFACTURERS AND SUPPLIERS

Carolina Stalite Company, Chuck Friedrich, RLA, ASLA, GRP

PO Box 1037 Salisbury, NC 28145 (800) 898-3772

# A.   Stalite G Fines from screening operation

Sieve Size        	% Retained

#4		  20-27%

#8                   47-65%

#16                 64-78%

#30		 75-85%

#50		  82-90%

#100		  87-95%

Fine Material   2.79-3.53 % passing  #200

B.	Approved Component

1. Compost must be certified and derived from a non-sewage sludge feedstock source. The addition of yard waste to the composting process must also meet certification requirements.

2.  Finished compost must be screened to minus 1/2”, protected, and free from any outside contaminants during and after screening and curing.

3. Metals and contaminants must meet or exceed US EPA Standard 40

C. Pine bark fines minus 3/8" screen

2.1	MIXING Procedure

A. Media Blending

Stalite Blend							75%

Approved Compost						15%

Pine Bark Fines						10 %